# TimberForm Separates™

No. 1601 White Water Raft

White Water Raft shall be TimberForm® model No. 1601 in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1.  MATERIALS

White Water Raft shall consist of platform members, platform support, spring assembly, handholds and assembly hardware.  Platform members shall be 4 x 6 and 6 x 6 Playground Equipment Grade free-of-heart-center (F.O.H.C.) Douglas fir timbers, selected by the equipment manufacturer for strength, durability, and appearance.  Spring assembly shall consist of four 9" high tension automotive-type coil springs and 1/4" thick steel top and bottom plates.  Handholds shall consist of 1-5/16" o.d. schedule 40 curved steel pipe with 1/4" thick mild steel brackets welded at each end.

2.  CONSTRUCTION

Timber decking shall be free of wane with all edges eased (rounded) to a 1/4 inch radius.  Springs shall be permanently welded to the plates to provide spring action.

3.  FINISH

Timber materials shall pressure treated with a non-toxic child safe preservative after all fabrication is completed.  Preservatives containing arsenic, pentachlorophenol, creosote or similar toxic chemicals as their active ingredient shall not be used.

Spring assembly shall be finished black with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.