# PipeLine Separates™

Model No. 1630-6-11-PL Spiral Spinner

Spiral Spinner shall be PipeLine® model No. 1630-6-11-PL in the color finish and quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Ste. 310, Portland, Oregon 97201-3464 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1.  MATERIALS

Spiral Spinner shal consist of support post assembly, top spindle assembly, spiral spinner assembly and base hub assembly.

Post assembly shall be 4-1/2" (o.d.) schedule 40 steel pipe with a minimum wall thickness of 7/32" in accordance with ASTM A-53, Type E, Grade A.  Thin wall tubing is not acceptable.  End of post shall be fitted with a cast aluminum hemi-dome end cap.

Spiral spinner assembly shall be 1-5/16" (o.d.)schedule 40 steel pipe permanently welded to top and bottom plate constructed of 3/16" thick mild steel plate and circular 1-5/8" (o.d.) schedule 40 steel pipe.  All welds shall comply with AWS standard D1.1.  All edges, ends, and welds shall be ground smooth by hand to a maximum grit of 36 and shotblasted to a uniform surface texture.

Base shall be embedded 2 feet – 9 inch and post shall be embedded 3 feet – 9 inch below finished grade in concrete footings as depicted on the erection drawings.  Actual concrete footing sizes can vary and depend on job site and climatic conditions.  Consult project engineer/owner for exact requirements.

2.  CONSTRUCTION

Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.

3. METAL FINISH

All metal parts other than those galvanized or stainless steel shall be finished with CASPAX-7™, a colorful, tough, opaque, exterior use powder coating.  Liquid, epoxy, or lead-containing powder coatings are not acceptable.