# TimberForm Embankment Slide

# Series 1640 Stainless Steel Embankment Slide Chute

Stainless Steel Embankment Slide Chute shall be TimberForm® Series 1640, in the length, color finish and quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, www.timberform.com.  Phone 800/547-1940.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1.  MATERIALS

Stainless steel embankment slide chute shall consist of entrance assembly, stainless steel slide chute, slide chute supports and attachment hardware.

Entrance assembly shall consist of transfer platform, posts, hand holds, and anti-spin bars at the top to help channel players into a safe, seated, sliding position.  Transfer platform shall be 11 gauge bent steel sheet perforated to allow water to drain.  Posts shall be 3” x 3” x 1/8” thick square steel tube.  Handles shall be 1-5/16” o.d. bent steel pipe. Anti-spin bars shall be 1 1/2” x 1 1/2” square steel tube.  Thin wall tubing will not be accepted.

Slide Chute stainless steel bedway assembly shall consist of a 1’-5 7/8" wide single sheet of 16-gauge T430 bright annealed stainless steel with side rails and shall include no laps or seams.  It shall be permanently attached to the side rails with "monobolts” and shall be reinforced from underneath by 16-gauge galvanized steel battens spaced no further than 4" on center.  Each side rail shall be aluminum "D" rail, shall extend 6" above the slide bedway, and have ends closed with the end caps permanently riveted in place.

Slide chute support assembly shall be constructed of 1" Schedule 40 galvanized steel pipe and 1/4” mild steel plate.  Chute shall slope approximately 30 degrees when properly installed.  In the exit area (bottom), side rails and assembly shall be curved to parallel grade as closely as possible, thereby slowing the player for safe discharge.

2.  CONSTRUCTION

Entrance assembly components shall be integrally connected and ship as one unit.  Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.

3.  FINISH

Metal components except those that are stainless steel or galvanized shall be color finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.

Additional hardware shall be provided in sufficient quantity to complete assembly of the TimberForm play equipment.  All hardware shall be non-ferrous, color finished with CASPAX-7, galvanized, or electrostatic zinc plated in accordance with the manufacturer's standard.