# TimberForm Separates™

### No. 1672 Double Arch Climber

Double Arch Climber shall be TimberForm® model No. 1672 in the quantity shown on the bill of materials or the project drawings.  Colors shall be the manufacturer's standard.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Ste. 310, Portland, OR 97201-5293 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

- MATERIALS

Double Arch Climber shall consist of two arches, 25 rungs, and four mounting brackets.

Wood arches shall be 3 x 9 glue-laminated Douglas fir timbers, premium appearance grade, dressed four sides with edges uniformly rounded and eased 1/4 inch.  Rungs shall be 1-5/16 inch (o.d.) schedule 40 steel pipe fitted with vandal resistant metal end caps.  Mounting brackets shall be 3/8 inch thick and 1/4 inch thick mild steel plate.

2. CONSTRUCTION

The top laminar shall be Alaska yellow cedar.  Arches shall be laminated with Type 1 adhesive suitable for wet service conditions.

3. FINISH

Douglas fir materials shall pressure treated with a non-toxic child safe preservative after all fabrication is completed.  Preservatives containing arsenic, pentachlorophenol, creosote or similar toxic chemicals as their active ingredient shall not be used.

Timber connectors shall be hot-dip galvanized and shall be concealed by close-fitting tapered hardwood plugs.

Rungs shall be finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.