# PipeLine Separates™

### No. 1992-12-00-PL Track Ride

Track Ride shall be PipeLine® model No. 1992-12-00-PL in the quantity shown on the bill of materials or the project drawings.  Colors shall be the manufacturer's standard.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Ste. 310, Portland, OR 97201-5293 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Track Ride shall consist of four posts, two end arch caps, trolley, heavy-duty track, support beam, and the necessary assembly and attachment hardware

Posts, end arch caps and beam shall be 4-1/2" (o.d.) schedule 40 steel pipe with a minimum wall thickness of 7/32". Thin wall tubing is not acceptable.

The trolley chassis shall be machined from solid 6061-T6 aluminum.  The four trolley wheels shall be polyurethane polyester with a 95A Durometer (very hard).  Wheels shall spin freely on permanently-lubricated ball bearings.

Two non-load bearing ultra high molecular weight (UHMW) wheels shall guide the moving trolley to buffer metal-to-metal contact between the trolley and the track.  Neoprene bumpers shall be fitted at both ends of the trolley chassis and at track ends to cushion the impact of the trolley and to minimize objectionable noise.

The handhold shall be formed from 1" diameter 6061-T6511 aluminum extrusion permanently welded to the chassis.  The handhold shall be perpendicular to trolley travel and knurled to facilitate the player's natural grip.

The track shall be one piece, formed from 13-gauge steel and bolted to a 4-1/2" o.d. Schedule 40 steel pipe beam.

2. CONSTRUCTION

Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs.

3. FINISH

All metal parts shall be color finished with CASPAX-7, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.