# PipeLine Separates™

### No. 1995-11-PL Accessible Ring Pull

Accessible Ring Pull shall be PipeLine® model No. 1995-11-PL in the quantity shown on the bill of materials or the project drawings.  Colors shall be the manufacturer's standard.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Ste. 310, Portland, OR 97201-5293 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Accessible Ring Pull shall consist of four posts and one ring pull assembly.

Steel posts shall be 4-1/2" (o.d.) schedule 40 steel pipe with a minimum wall thickness of 7/32". Thin wall tubing is not acceptable.  Exposed ends of posts shall be fitted with a cast aluminum (384 alloy) hemi-dome end cap permanently adhered in place.  Easily vandalized plastic and/or friction fit end caps are not permitted.

Rail with rings shall consist of two triangular aluminum-alloy trapeze rings and one 1-5/16" (o.d.) schedule 40 pipe rail.  Rail shall be connected to posts by cast aluminum (384 alloy) two-piece attachment collars, formed to recess bolt fastener.  Each collar set shall include two vandal-resistant socket-head cap screws with nuts and two 1/4" aluminum hammer-drive rivets.

2. CONSTRUCTION

Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs.

3. FINISH

All steel parts shall be color finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.