# PipeLine Separates™

### No. 1996-1-67-PL Chinning Bar

Chinning Bar shall be PipeLine® model No. 1996-1-67-PL in the quantity shown on the bill of materials or the project drawings.  Colors shall be the manufacturer's standard.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Ste. 310, Portland, OR 97201-5293 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Chinning Bar shall consist of a one post and one bar.

Steel post shall be 4-1/2" (o.d.) schedule 40 steel pipe with a minimum wall thickness of 7/32". Thin wall tubing is not acceptable.  Exposed end of post shall be fitted with a cast aluminum (384 alloy) hemi-dome end cap permanently adhered in place.  Easily vandalized plastic and/or friction fit end caps are not permitted. Bar shall be smoothly formed 1-5/16" o.d. schedule 80 steel pipe.

Bar shall be connected to post by cast aluminum (384 alloy) two-piece attachment collar, formed to recess bolt fastener.  Collar set shall include two vandal-resistant socket-head cap screws with nuts and two 1/4" aluminum hammer-drive rivets.

2. CONSTRUCTION

Ends of springs shall be closed and ground smooth prior to finishing.  Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs.

3. FINISH

All metal parts shall be color finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.