# TimberForm Separates™

Series 3880 Spring Rider (straddle type)

No. 3881-01-XW Cycle, No. 3884-01-YW Sea Horse, No. 3889-01-XW Pony

Spring Rider shall be TimberForm® Series 3880 in the quantity shown on the bill of materials or the project drawings.  Colors shall be the manufacturer's standard.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Portland, OR 97201-5293 U.S.A.  Phone 503/223-1157.

1. Materials

Spring Rider shall consist of panels, spring, handle/footrest assembly, and assembly hardware. Standard mounting shall be -E embedment (permanent).  Optional: -P pedestal (fixed surface) mount.

Panels shall be manufactured from 3/4" thick tri-layered high-density compression molded polyethylene.  Exposed panel edges shall be eased (rounded) with 3/16" radius.  Polyethylene shall be formulated for optimum U.V. stability and color retention.

Spring shall be manufactured from 25/32" (20 mm) thick wire.  Spring plates shall be a deep drawn product contoured to match the spring and form a single unit with finger-pinching protection.  The spring shall be guaranteed by the manufacturer against breakage for five years.

Handles/footrests shall be smoothly formed of 1-5/16" (o.d.) schedule 40 steel pipe.

Embedment (-E) mount rider shall include three 1-5/16" (o.d.) schedule 40 steel pipe legs which embed in concrete.  Optional pedestal (-P) mount rider shall have three 3/4" diameter holes in the base plate for anchor bolts (supplied by installing contractor).

2. Construction

Individual panel layers shall have homogenous colored throughout with the interior layer being one color and two exterior layers a second color.  Ends of spring shall be closed and ground smooth prior to finishing.  Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.

3. Finish

Spring and handles/footrests shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Spring shall be zinc phosphate coated prior to powder-coating.