# Classic TimberForm™

# No. 4500-008 – Classic TimberForm® Play Stack

Play Stack shall be Classic TimberForm® model No. 4500-008 in the quantity shown on the bill of materials or the project drawings. Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201-3464 U.S.A.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Play Stack shall consist of wood logs, steel support posts, and attachment hardware.

Logs shall be coastal Douglas fir (Pseudo-tsuga menziesii), free-of-heart-center (F.O.H.C.) selected by the equipment manufacturer for strength, durability, and appearance.  To assure long, useful life, timbers containing the heart center of the log shall not be accepted.

All timbers shall be fine-grained, with at least 80 percent of the pieces possessing eight annular rings to the inch, the remainder having at least six rings to the inch.  There shall be no loose knots, knotholes, shake, unsound wood, white specks or honeycomb allowed. Except as noted, other characteristics and limiting provisions are in accordance with Paragraph 131-A "Standard Grading Rules for West Coast Lumber".

Steel support posts shall consist of 2 1/2” x 2 1/2” x. 0.188 thick square steel tubing with permanently welded 1/4” thick steel support bracket. Support posts and brackets shall be CASPAX-7( finished in accordance with Section 3.0.

Additional hardware shall be provided in sufficient quantity to complete assembly of the TimberForm play equipment.  All hardware shall be hot dip galvanized or stainless steel in accordance with the manufacturer's standard.

2.  CONSTRUCTION

Logs shall be lathe-turned to a constant diameter of 11” with exposed ends trimmed and eased.

Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs.

3. FINISH

Timber materials shall be pressure treated with a non-toxic child safe preservative after all fabrication is completed.  Preservatives containing arsenic, pentachlorophenol, creosote or similar toxic chemicals as their active ingredient shall not be used.

Metal components, other than those galvanized or stainless steel, shall be color finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.