# Classic TimberForm

# No. 4500-503 Classic TimberForm Stepping Column® Cluster

Stepping Column® Cluster shall be Classic TimberForm® model No. 4500-503 in the quantity shown on the bill of materials or the project drawings. Manufacturer, Columbia Cascade Company, www.timberform.com. Phone 800/547-1940.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Stepping Column Cluster shall consist of wood columns and attachment hardware.

Columns shall be 12 x 12 (nom.) coastal Douglas fir (Pseudo-tsuga menziesii), free-of-heart-center (F.O.H.C.) selected by the equipment manufacturer for strength, durability, and appearance.  To assure long, useful life, timbers containing the heart center of the log shall not be accepted.

All timbers shall be fine-grained, with at least 80 percent of the pieces possessing eight annular rings to the inch, the remainder having at least six rings to the inch. Timbers with loose knots, knotholes, shake, unsound wood, wane, planer skips, white specks or honeycomb will not be accepted. Except as noted, other characteristics and limiting provisions are in accordance with Paragraph 131-A "Standard Grading Rules for West Coast Lumber".

2. Construction

Timber columns shall be smoothly dressed to a net size of 11 ¼ inches x 11 ¼ inches with all edges eased (rounded) to a ¼ radius. Column tops shall be chamfered 3/4” all edges.

Columns shall be connected using 5/8” dia. x 14” hot dipped galvanized lag screws. Hardware shall be provided in sufficient quantity to complete assembly of the Stepping Column Cluster.

3. Finish

Stepping Column Cluster shall be pressure treated with a non-toxic preservative after all fabrication is completed.  Preservatives containing arsenic, pentachlorophenol, creosote or similar toxic chemicals as their active ingredient shall not be used.