TimberForm RePlay Playground Equipment

PLAY STRUCTURE

The play structure shall be TimberForm RePlay® as manufactured by Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201-3464 U.S.A.

# GENERAL

Deck modules shall be 3 foot 10 inches on center in accordance with the following specifications.  Model numbers are for apparatus only and do not include supporting structure or required safety rails unless noted.  All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1.0  PLASTIC TIMBERS

All play equipment plastic timber components shall be 100% post-consumer extruded high density polyethylene (H.D.P.E.), cedar colored, selected by the equipment manufacturer for strength, durability and appearance.  Molded recycled plastic timbers have unacceptable surface texture and shall be rejected.

1.1  Posts

Posts shall be smoothly extruded to a net size of 5-1/4 inches x 5-1/4 inches with all edges eased (rounded).  Post tops shall be chamfer-sawn 45 degrees.

1.2  Beams

Beams shall be smoothly extruded to a net size of 5-1/4 inches x 5-1/4 inches, edges eased (rounded).  Precision notches shall be simultaneously machined into each beam end to a tolerance of 1/32 inch in order to achieve and maintain structural integrity of the erected play structure.  All beam bolt holes shall be drilled and counter-bored to recess bolt heads beneath the beam face.

1.3  TimGrip™ Fasteners

TimGrip stainless steel bolts are furnished as standard.  TimGrip hardware has unique thread geometry especially designed, tested and proven to securely and permanently grip recycled HDPE plastic.  Ferrous or ordinary lag screw fasteners shall not be accepted for HDPE connections.

1.4  Quality Control

Inspectors shall examine each plastic timber component for correct fabrication, fastener hole alignment, and for smooth end, edge, and face treatment.

2.0  METAL MATERIALS

Unless otherwise noted, all rails shall be 1-5/16 inch (o.d.) schedule 40 steel pipe in accordance with ASTM A-53, Type E, Grade A.  Thin wall tubing is not acceptable.  Steel plate shall be in accordance with ASTM A-36.  All steel parts shall be CASPAX-7( finished in accordance with Section 3.0.

2.1  Fabrication

All welds are to comply with AWS standard D1.1.  All edges, ends, and welds shall be ground smooth by hand to a maximum grit of 36 and shotblasted to a uniform surface texture.

2.2  Quality Control

Inspectors shall examine metal components for correct fabrication, fastener hole alignment, and smoothness.

2.3  Additional Hardware

Additional hardware shall be provided in sufficient quantity to complete assembly of the TimberForm play equipment.  All hardware shall be non-ferrous, color finished with CASPAX-7, galvanized, or electrostatic zinc plated in accordance with the manufacturer's standard.

3.0   METAL FINISH

All metal parts other than those galvanized or stainless steel shall be finished with CASPAX-7, a colorful, tough, opaque, exterior use powder coating.  Liquid, epoxy, or lead-containing powder coatings are not acceptable.  The CASPAX-7 color shall be the manufacturer's standard or as selected by the owner's representative and designated on the project plans and/or specifications.

3.1  Cleaning

Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., then chemical cleaning in accordance with TT-C-490C, Methods I and III.

3.2  Phosphate Application

After cleaning, the metal substrate shall receive a corrosion-inhibiting iron phosphate coating in accordance with TT-C-490C, Type II, before application of the final color coat.

3.3  Powder Application

The coating powder shall be uniformly applied by the electrostatic method to a thickness of six mils.  Promptly after the application of the powder, the coating shall be oven-cured at 400 degrees Fahrenheit to chemically bond the finish to the substrate and to render the color coated surface resistant to abrasion, impact, household chemicals, weathering and rusting.

3.4  Chronological Importance

For a corrosion-inhibiting agent to be effective, all fabrication including cutting, coping, grinding, and welding must be completed before application of the corrosion-inhibiting agent.  Corrosion-inhibiting agents applied prior to fabrication are not acceptable.

3.5  Quality Control

The applicator shall test the finish of each lot for correct millage, chemical resistance,  hardness, and internal bond in accordance with established industry standard test methods.

Records of this quality control procedure shall be made and retained for two years.

4.0  POLYETHYLENE MATERIALS

Polyethylene shall be linear medium density with the maximum ultraviolet degradation inhibitors and may be specified in yellow or tan.

4.1  Fabrication

Plastic components shall be one-piece, rotationally molded polyethylene.  Each component shall be free of burrs, warpage, cupping, and other irregularities.  Mold parting lines and all edges shall be trimmed and finished smooth.

4.2  Finish

Exterior surfaces shall be textured to camouflage any scratches or markings.  Surfaces intended for passage or sliding shall be finished smooth.

4.3  Quality Control

Inspectors shall examine each plastic component for correct fabrication including:  wall thickness, cure, texture, fastener hole alignment, and color uniformity.

5.0  Brown Thermoplastic-Coated Perforated Steel SofDeks

SofDeks shall be manufactured of 11 gage (.125" thick) perforated mild steel plate.  Each deck unit shall be reinforced with 1/4 inch thick mild steel bar as necessary to insure structural integrity.  Corners of each deck shall fit closely with support posts and allow for attachment to posts with supplied lag screws.  No sharp metal edges shall be exposed.

All fabricated metal components to be textured thermoplastic coated shall have edges and ends deburred and ground smooth prior to being finished.  Preparation of the steel substrate shall incorporate mechanical cleaning to remove heavy mill scale, varnish, rust, grease, etc.; then a prime coat shall be applied.  The ultra-violet stabilized thermoplastic coating shall be applied by the electrostatic process to pre-heated substrate to a thickness of approximately 30 mils then allowed to cure before handling.  Final Durometer (hardness) shall be 52 on the D Shore scale in accordance with ASTM D 2240.

(Alternate) 5.0 Recycled Plastic Decks with Steel Frames

[Recycled plastic decks shall have 2 x 6 (nominal) wood-polymer composite planks.  The majority of the material shall be from reclaimed plastic and waste wood and it shall be 100% recyclable.  No virgin wood shall be used.

Standard color selection shall be light brown.  There shall be only slight color variations amongst the supplied product.  Each deck member shall be smooth on four sides, free of splinters, resistant to insect damage, rot, checking, splitting, and U.V. damage.

Deck frame shall be constructed from 1/4" x 2-1/2" mild steel bar and 2" x 1" x 3/16" mild steel channel, formed into a frame to accept the 2 x 6 deck timbers. Corners of each deck shall fit closely with support posts and allow for attachment to posts with supplied lag screws.  No sharp metal edges shall be exposed.  Frame shall have edges and ends deburred and ground smooth prior to powder coating with CASPAX-7 in accordance with Section 2.0.  Timbers shall attach to the frame with No. 14 x 1-1/4" stainless steel pan head screws.]

6.0  INSTALLATION INSTRUCTIONS AND AIDS

To guide installation, each TimberForm RePlay structure shall be accompanied by bills of materials, written instructions, and an erection plan view drawing to be furnished prior to or with the delivery of the play structure.  To facilitate assembly, each part shall be indelibly stenciled with an easily-read identification number keyed to the bills of material and erection drawings.  All components shall be shipped unitized, protectively wrapped, banded for mechanical handling and ready for assembly.  The timber structure shall be installed entirely upon virgin soil or firm compacted grade.