# TimberForm Separates™

No. 1628-12-12 Curved Steel Balance Beam

Curved Steel Balance Beam shall be TimberForm® model No. 1628-12-12 in the color finish and quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland, OR 97201 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Curved Balance Beam assembly shall consist of a 3" x 2" x 12'-0" rectangular steel beam and three 2-3/8" (o.d.) schedule 40 steel pipe legs permanently welded in place to form a one-piece assembly. Beams shall have two 30-degree dog-legs.

2. CONSTRUCTION

Welds shall be smooth and continuous with no gaps or pin holes.  Final product shall be free of weld spatters and burrs.

3. FINISH

Balance beam shall be color finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.  After coating with CASPAX-7, the walking surface of the beam shall have a matching slip-resistant sand surface applied.