# PipeLine Separates™

### No. 1918-00-03-PL Tunnel Crawl, Stainless Steel

Tunnel Crawl, Stainless Steel shall be PipeLine® model No. 1918-00-03-PL in the quantity shown on the bill of materials or the project drawings.  Colors shall be the manufacturer's standard.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Ste. 310, Portland, OR 97201-5293 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Tunnel Crawl, Stainless Steel shall consist of four posts, two metal panels, one tube section, attachment rails, and assembly hardware.

Steel posts shall be 4-1/2" (o.d.) schedule 40 steel pipe with a minimum wall thickness of 7/32". Thin wall tubing is not acceptable.  Exposed ends of posts shall be fitted with a cast aluminum (384 alloy) hemi-dome end cap permanently adhered in place.  Easily vandalized plastic and/or friction fit end caps are not permitted.

Panels shall be ¼ thick steel with twelve 3/8” thru holes for attachment of tunnel.

Tunnel shall be manufactured of 14-gauge Type 304 polish stainless steel formed into a two-foot diameter cylinder.  All seams shall be ground and buffed smooth.  Ends shall be hemmed to eliminate sharp edges.

Rails shall be constructed of 1-5/16" o.d. schedule 40 steel pipe and connected to posts by cast aluminum (384 alloy) two-piece attachment collars, formed to recess bolt fastener.  Each collar set shall include two vandal-resistant socket-head cap screws with nuts and two 1/4" aluminum hammer-drive rivets.

2. CONSTRUCTION

Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs.

3. FINISH

Metal components, other than those galvanized or stainless steel, shall be color finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.