# PipeLine Separates™

### No. 1919-00-01-PL Tunnel Crawl

Tunnel Crawl shall be PipeLine® model No. 1919-00-01-PL in the quantity shown on the bill of materials or the project drawings.  Colors shall be the manufacturer's standard.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Ste. 310, Portland, OR 97201-5293 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Tunnel Crawl shall consist of four posts, two double-walled plastic panels, one tube section, attachment rails, and assembly hardware.

Steel posts shall be 4-1/2" (o.d.) schedule 40 steel pipe with a minimum wall thickness of 7/32". Thin wall tubing is not acceptable.  Exposed ends of posts shall be fitted with a cast aluminum (384 alloy) hemi-dome end cap permanently adhered in place.  Easily vandalized plastic and/or friction fit end caps are not permitted.

Panels and tube section shall be shall be one-piece, rotationally molded polyethylene.  Panels shall be 38" wide x 38" high with 1/4" wall thickness.  Each panel face shall have a relieved radial patterned surface for structural integrity and fine appearance.  Tube section shall be nominal 4 feet long with ¼” wall thickness.  Panels and tube section shall be TAN or YELLOW in color.

Rails shall be constructed of 1-5/16" o.d. schedule 40 steel pipe and connected to posts by cast aluminum (384 alloy) two-piece attachment collars, formed to recess bolt fastener.  Each collar set shall include two vandal-resistant socket-head cap screws with nuts and two 1/4" aluminum hammer-drive rivets.

2. CONSTRUCTION

Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs.

3. FINISH

Metal components, other than those galvanized or stainless steel, shall be color finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.