# PipeLine Separates™

### No. 1995-12-81-PL Pivot-Pad Bridge

Pivot-Pad Bridge shall be PipeLine® model No. 1995-12-81-PL in the quantity shown on the bill of materials or the project drawings.  Colors shall be the manufacturer's standard.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Ste. 310, Portland, OR 97201-5293 U.S.A.  Phone 503/223-1157.

GENERAL

All fabrication shall take place in an enclosed factory environment by personnel experienced in the manufacture of children's play apparatus.

1. MATERIALS

Pivot-Pad Bridge shall consist of four posts, two tee-frames, and one beam with integrally mounted hangers and seven pivot pads.

Posts, tee-frames and beam shall be 4-1/2" (o.d.) schedule 40 steel pipe with a minimum wall thickness of 7/32". Thin wall tubing is not acceptable.  Exposed ends of posts shall be fitted with a cast aluminum (384 alloy) hemi-dome end cap permanently adhered in place.  Easily vandalized plastic and/or friction fit end caps are not permitted.

Pivot-pads shall be constructed of 3/16" thick mild steel plate, circular 1" (o.d.) schedule 40 steel pipe and ¼” galvanized chain embedded in concrete with a piece of No. 4 re-bar (supplied by installing contractor).

2. CONSTRUCTION

Welds shall be smooth and continuous with no gaps or pinholes.  Final product shall be free of weld spatters and burrs.

3. FINISH

All metal parts shall be color finished with CASPAX-7™, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.

Pivot-Pad Bridge shall consist of a pivot-pad assemblies attachment to a steel horizontal beam and support posts constructed of 4-1/2 inch (o.d.) schedule 40 steel pipe in accordance with Section 1.0. Pivot-pad shall be constructed of 3/16" thick mild steel plate, circular 1" (o.d.) schedule 40 steel pipe and ¼” galvanized chain embedded in concrete with a piece of No. 4 re-bar (supplied by installing contractor).